## Slide 1: Simulation of production process-related adhesive damage of adhesively bonded multi-material body in white
Suba Siva Chandran, Kalimuthu, 28.05.2020

## Slide 2: Contents
  Introduction
  Industrial process and problem description
  Motivation and objective
  Overview of material properties
  Workflow of the simulation
          Results
          Conclusion and future work

## Slide 3: Introduction
What is a multi material BIW?
Stage in manufacturing process
Components joined together
27% of a car’s curb weight
Lightweight materials in a BIW
Advantages
Increases fuel economy
Reduces overall weight
Can be safer
Improves handling of the car
Multi-material BIW [1]

## Slide 4: Contents
  Introduction
  Industrial process and problem description
  Motivation and objective
  Overview of material properties
  Workflow of the simulation
          Results
          Conclusion and future work

## Slide 5: Industrial process and problem description
Pressing
Assembling
Paint pre-treatment
Final curing
Cathodic dip paint oven
185°C
15 mins(approx.)
Cathodic dip painting
Relative displacements [3]
Overview of the industrial process [2]

## Slide 6: Industrial process
Heated to 185°C and cooled down to room temperature
Several zones connected in series with different temperatures
Homogenous heating must be ensured in mixed construction bodies
Step shaped heating and same applies to cooling profile
Freshly painted car body positioned in paint-drying oven for curing [4]
Schematic representation of the temperature curve in a multi-material dryer process [2]

## Slide 7: Problem description
Relative displacements in flanges due to different expansion coefficients
It describes the resulting mechanical stress on bonded joint and joining partner
1
2
Heating phase
3
Holding phase
4
Cooling phase
Temperature curve CDP dryer with resulting relative shift in the adhesive flange during the heating and cooling zone [2]
Adhesive fracture [3]
Adhesive crack [3]
Delta Alpha problem
Adhesive failures

## Slide 8: Contents
  Introduction
  Industrial process and problem description
  Motivation and objective
  Overview of material properties
  Workflow of the simulation
          Results
          Conclusion and future work

## Slide 9: Motivation and objective
Objective
To investigate the influence of thermal expansion coefficients of different materials
A vehicle model of Toyota Camry available at GNS mbH, Braunschweig is used
To simulate the adhesive layer damage using FEM software ABAQUSTM
Porsche 911 BIW, Blue – Aluminium / Red, Orange, Yellow and Green – Steel [2]
Motivation
CO2 limit value curve is planned for new vehicles
No more than 95 g/km of CO2 by 2021
Porsche 911 BIW - A mixed construction concept

## Slide 10: Contents
  Introduction
  Industrial process and problem description
  Motivation and objective
  Overview of material properties
  Workflow of the simulation
          Results
          Conclusion and future work

## Slide 11: Overview of material properties
Thermal properties
Mechanical properties
ρ, k, c
E, ν, α, εp
Film coefficient


Damage model for adhesive


Steel
Aluminium
Spot weld
Adhesive
Material properties needed
Steel hatprofile
Aluminium plate

## Slide 12: Validation of film coefficient
Experimental setup of cooling process
DC01 Steel hatprofile
Experiment | Room temperature [°C]
Experiment 1 | 23
Experiment 2 | 20.5
Experiment 3 | 18
DC01 Steel hatprofile
Room temperatures of the experiments conducted

## Slide 13: Validation of film coefficient
Steel hatprofile ABAQUS TM model
Property | Symbol | Unit | Steel
Density | ρ | ton mm−3 | 7.85e-9
Thermal conductivity | k | mW mm−1K −1 | 52
Specific heat capacity | c | mJ ton−1K −1 | 0.48e9
Dimension of Steel hatprofile FE model
Temperature measurement points
Thermal properties used for DC01 Steel simulation

## Slide 14: Validation of film coefficient
Steel hatprofile ABAQUS TM model – Thermal analysis
23°C – Sink temperature
Thermal analysis of Steel hatprofile
180°C – Initial condition

## Slide 15: Validation of film coefficient
Experiment vs Simulation curves
Experiment vs simulation cooling rate of DC01 Steel hatprofile
Temperature-dependent film coefficients finalized for Steel material
Temperature-dependent film coefficients obtained from FE simulations

## Slide 16: Validation of film coefficient
Aluminium plate ABAQUS TM model
Property | Symbol | Unit | Aluminium
Density | ρ | ton mm−3 | 2.71e-9
Thermal conductivity | k | mW mm−1K −1 | 237
Specific heat capacity | c | mJ ton−1K −1 | 0.91e9
Dimension of Aluminium plate FE model
Temperature measurement points
Thermal properties used for EN-AW-6082 Aluminium simulation
All dimensions are in mm
All dimensions are in mm

## Slide 17: Validation of film coefficient
Finalized simulation film coefficient [mW mm−2K−1 ] | Temperature [°C]
0.008 | 20
0.023 | 80
Temperature-dependent film coefficients finalized for Aluminium material
Experiment vs simulation cooling rate of EN-AW-6082 Aluminium plate
Room temperature : 26°C

## Slide 18: Mechanical properties
Steel and Aluminium
Validated with data according to
DIN EN ISO 527

## Slide 19: Mechanical properties
Thermal properties used for BM1480 V203 adhesive
Temperature-dependent thermal expansion coefficient used for BM1480 V203 adhesive
Thermal expansion coefficient of spot weld – 0.0004 per Kelvin
Spot weld
Adhesive
One component heat curing epoxy- based
BETAMATETM 1480V203

## Slide 20: Mechanical properties
Damage model of adhesive in ABAQUSTM
Mechanical parameters of a bilinear traction separation law [5]
Energy release rates [5]
Strength and stiffness parameters [5]

## Slide 21: Contents
  Introduction
  Industrial process and problem description
  Motivation and objective
  Overview of material properties
  Workflow of the simulation
          Results
          Conclusion and future work

## Slide 22: Workflow of the simulation
Phase 1:
Preprocessing the model
Material data checks
Establishing FE representation of spot weld connections
Surface SET creation
Phase 2:
Importing the model
Creating necessary BC’s
Transient thermal analysis
Subsequent structural analysis
Workflow of the simulation of cooling process

## Slide 23: Workflow in ANSATM pre-processor
PAM-CRASH version to ABAQUS version
Adhesive damage results can be used in the crash simulation
Hybrid joined aluminium panel floor members on a steel platform
Around 5000 (approx.) spot welds and few adhesive connections
Toyota Camry model
Aluminium parts in the entire car model
Aluminium flanges adhesively bonded to the steel platform

## Slide 24: Workflow in ANSATM pre-processor
Preprocessing procedure
Process flowchart for pre-processing
Connection entities | PAM-CRASH | ABAQUS
Spot weld | PLINKS | DYNA spot weld
Finite element representations of the connection entities
Example of two components to be tied together [6]

## Slide 25: Workflow in ABAQUSTM
Two fields has to be determined in thermo-mechanical analysis
One field influences the other or both can influence each other
Temperature
Displacement
Load
Can be solved by uncoupled heat transfer and then a displacement/stress analysis
In this problem, temperature does not depend on stress analysis
This is a common example of sequential multiphysics workflow
Sequentially coupled thermal stress analysis

## Slide 26: Thermal-stress analysis in ABAQUSTM
Simulation procedure in ABAQUSTM
Part
Property
Step
Interaction
Load
Mesh
Job
Thermal
Mechanical
ρ, k, c
E, ν, α, εp
Heat transfer
2400 seconds
Static, general
2400 seconds
1. Film condition
2. Suppress MPC
Redefine MPC
Initial condition
180°C
Nodal temp results
DS4, DS3, DC3D8
S4R, S3, C3D8, COH3D8
Thermal analysis results
Displacement, SDEG

## Slide 27: Contents
  Introduction
  Industrial process and problem description
  Motivation and objective
  Overview of material properties
  Workflow of the simulation
          Results
          Conclusion and future work

## Slide 28: Results
Temperature distribution during cooling process
Temperature distribution is inhomogenous
Variation in thickness of the components and geometry
Right midrail – (Thickness: 2.628mm)
Steel platform – (Thickness: 0.75mm)
Temperature distribution after 527 seconds
Temperature difference between thin and thick shell parts
1
2
2
1

## Slide 29: Results
Temperature variation of components connected by spot weld
Measurement point to illustrate temperature variation
Temperature difference of upper rail rear and upper rail top
Upper rail top and rear parts are investigated
Mild difference of about 1°C
Reasonable and precisely accurate

## Slide 30: Results
Overall displacement during cooling process
Maximum displacement is found in the roof cross members
Body has less than 4mm displacement overall

## Slide 31: Results
Displacement of steel platform during cooling
Displacement in X-direction
Displacement in Z-direction
Entire vehicle starts to contract during cooling
Displacement along x-direction leads to buckling of floor front
A peak value of 2mm displacement along the transverse direction
Thickness of the components

## Slide 32: Results
Deformation of the aluminium flange
Element deletion based upon damage
Maximum degradation is 1
Crossing of adhesives leads to the maximum degradation
Scaled by a factor of 20
Scaled by a factor of 15

## Slide 33: Results
Stiffness degradation of adhesive in other regions
SDEG of adhesive in B-pillar
SDEG of adhesive in rear outer panel
No degradation in the spot weld regions within adhesive in B-pillar
Minimal stiffness degradation in the adhesive connecting floor trunk

## Slide 34: Contents
  Introduction
  Industrial process and problem description
  Motivation and objective
  Overview of material properties
  Workflow of the simulation
          Results
          Conclusion and future work

## Slide 35: Conclusion and scope for future work
Conclusion
A method has been identified for simulation
Offers possibility of heat transfer through spot welds in thermal analysis
A process history of the behavior of adhesive can be established
The critical spots of the BIW structure can be determined
Future work
An experimental verification of the adhesively bonded BIW structure numerically calculated in this work is desirable
Long running time of mechanical simulation should be investigated

## Slide 36
Thank you for your attention

## Slide 37: References
https://www.linkedin.com/pulse/body-white-biw-design-fundamentals-part1-mahm%C3%BCd-hosseinjani
Robert Georg Dietrich. Analyse der Wärmeausdehnungs-Inkompatibilität bei
Klebverbindungen aus CFK, Stahl und Aluminium bei der Fertigung einer lackierten Karosserie (2017). PhD thesis, Technische Universität München, Germany.
Numerische abschätzung von eigenspannungen und bauteilverformungen in gesamtfahrzeugmodellen beim kleben im karosseriebau. Paderborner Symposium Fügetechnik (2006).
https://www.theseus-fe.com/ths_content/publications/slides/20061129_slides_kleben-im-karosseriebau_prozess-simulation_de.pdf
Theseus FE.
https://www.theseus-fe.com/simulation-software/paint-dryer-simulation

## Slide 38: References
5. Niklas Günther, Michael Griese, Elisabeth Stammen, and Klaus Dilger.(2018) Modeling of adhesive layers with temperature-dependent cohesive zone elements for predicting adhesive failure during the drying process of cathodic dip painting.
6. ABAQUS manual V6.6 https://classes.engineering.wustl.edu/2009/spring/mase5513/abaqus/docs/v6.6/books/usb/default.htm?startat=pt08ch28s03aus107.html#usb-cni-ptiedconstraint