## Slide 1: Simulation of process induced deformations of fusion bonded hybrid components and potential analysis in a car model
Suba Siva Chandran, Kalimuthu, 22.09.2021
[5]

## Slide 2: Introduction
[5]
Tunnel upper area in BMW M7 [6]
Spaceframe made up of 79% Aluminium and 13% CFRP
Upper roof rail in BMW M7 [6]
Audi R8 spaceframe rear wall is made up of CFRP and has high tensile strength of about 2000 MPa
Freshly painted car body positioned in paint-drying oven for curing [7]
Different variables during paint drying process [11]
[8]
Lightweight concept in automotive
Industrial process
Steel – 1.3e-5
Aluminium – 2.4e-5
GFRP – 1.77e-5

## Slide 3: Problem description
Goal:
To devise a process simulation method for fusion bonding incorporated adhesive joining process which involves hybrid materials in the FEM software ABAQUSTM
To predict the stresses in the adhesive layer after the paint dryer process as a result of CTE mismatch
What is fusion bonding or co-curing?
Fusion bonding
+
Adhesive joining
with epoxy film
=
How much would be the strength of the hybrid joint ?
Illustration of fusion bonding process [1]
Bonding strength of co-cured vs co-cured with adhesive [2]

## Slide 4: Motivation and Objective
Motivation:
Multi-material system plays a crucial role during crash and a superior choice over traditional metal sheet
Combining the advantages of fusion joining and adhesive bonding methods
To analyze the structural efficiency of the hybrid joint
Objective:
To investigate the influence of thermal expansion coefficients of different materials
To simulate the process and predict adhesive layer damage using FEM software ABAQUSTM
To transfer the process simulation to a potential component in car model
Hybrid B-pillar assembly made of Steel and CFRP in BMW M7 [4]

## Slide 5: Contents
  Hybrid plate overview and material model requirement
  Workflow and Simulation principle
          Hybrid plate process simulation
          Structural test and its validation
          Potential analysis in Toyota Camry
          Conclusion and future work
Hybrid front bumper [3]
&
What parameter has to be evaluated for cooling process ?
3-point-bend test fixture [12]
Simulation method transfer

## Slide 6: Contents
  Hybrid plate overview and material model requirement
  Workflow and Simulation principle
          Hybrid plate process simulation
          Structural test and its validation
          Potential analysis in Toyota Camry
          Conclusion and future work

## Slide 7: Hybrid plate overview and material model requirement
Thermal properties
Mechanical properties
ρ, k, c
E, ν, α, εp
Film coefficient


Damage model for adhesive


Steel
GFRP-PA6 (Twill fabric - RG600(x)/47% Roving Glass – PA 6 Consolidated Composite Laminate from LANXESS AG)
Adhesive (Modified Epoxy film adhesive from Hexcel)
Support plate
Hybrid plate manufacturing setup

## Slide 8: Contents
  Hybrid plate overview and material model requirement
  Workflow and Simulation principle
          Hybrid plate process simulation
          Structural test and its validation
          Potential analysis in Toyota Camry
          Conclusion and future work

## Slide 9: Workflow
GFRP heated above melting point in the oven
Joined together with Steel, adhesive by heat press
Allow to cool down from 150°C to RT
Hybrid plate
Goal:
To manufacture the hybrid plate and simulate the cooling procedure to evaluate the stresses in adhesive layer as a result of CTE mismatch
To perform the 3-point-bending tests to assess the strength of hybrid joint as it is the common mode of deformation during car crash
Process
Structural

## Slide 10: Simulation principle
Process
Structural
Temperature recording using thermocouple
Process simulation transfer
Nodal temperature
Displacements
Steel
GFRP
Goal:
Film condition evaluation must be done to simulate the cooling process

## Slide 11: Contents
  Hybrid plate overview and material model requirement
  Workflow and Simulation principle
          Hybrid plate process simulation
          Structural test and its validation
          Potential analysis in Toyota Camry
          Conclusion and future work

## Slide 12: Hybrid plate process simulation
Steel
Goal:
To record the temperature distribution of the individual components of the hybrid plate and to compare the results with FE results to obtain a justification
Cooling experiment for the Steel component of the hybrid plate
Steel
Method
Free convective cooling of CFRP
Experimental Method
Free convective cooling of Steel plate
Material
Experimental duration
1225 seconds
Temperature
Initial temperature – 180°C
Steel plate (Thickness - 1.63 mm)
Geometry & Measurement points
a = 229.5 mm, b = 229.5 mm
Film condition obtained for individual components of hybrid plate

## Slide 13: Hybrid plate process simulation
Steel
Support plate
GFRP
The film condition for different components of hybrid plate were validated with the experimental results and found a good correlation and therefore to be used for the process simulation

## Slide 14: Hybrid plate process simulation – Thermal analysis results
The temperature distribution on the lower surface of the GFRP is stagnated since it is fixed firmly to the support plate
Dimensions: GFRP, Steel – 230 x 230
Adhesive – 230 x 170
Support plate – 300 x 230
After 485 seconds

## Slide 15: Hybrid plate process simulation – Mechanical analysis results
An average of 45% stiffness degradation is found within the adhesive
Also, in many regions the damage initiation criterion had already exceeded which indicates that more damage is likely
Steel adherend displaces in out-of-plane direction in production of DCB hybrid plate

## Slide 16: Process validation – Mechanical analysis results
The process has been validated by checking the deflections with the help of linear extensometer
Experimental setup of process validation
Dimensions: GFRP, Steel, BA – 200 x 20
Support plate – 300 x 230

## Slide 17: Contents
  Hybrid plate overview and material model requirement
  Workflow and Simulation principle
          Hybrid plate process simulation
          Structural test and its validation
          Potential analysis in Toyota Camry
          Conclusion and future work

## Slide 18: Structural test and its validation
The strength of the hybrid specimen is tripled whereas for the 3-PB of Steel specimen alone it withstands max.force of only 0.55 kN
There were some internal plasticity effects within GFRP which is also not modelled in the simulation

## Slide 19: Contents
  Hybrid plate overview and material model requirement
  Workflow and Simulation principle
          Hybrid plate process simulation
          Structural test and its validation
          Potential analysis in Toyota Camry
          Conclusion and future work

## Slide 20: Potential analysis in Toyota Camry
Pole
Barrier
ODB
SOL


## Slide 21: Hybrid component in car model
3mm patch variant
Version | Property name | Mass [kg] | Thickness [mm]
Basis | Floorpanelxmember | 2.09 | 2
V097 | Floorpanelxmember | 1.67 | 1.6
 | Patch | 0.163 | 3
Mass reduction of 0.52 kg/car

## Slide 22: Plasticity and Intrusion comparison
Basis
Basis
Patched variant
Patched variant
-375.23 mm
-368.37 mm

## Slide 23: Spot weld failure comparison
Basis
Failures occur in time period of 15 ms
Patched variant
Failures occur in time period of 25 ms
Spotwelds were added additionally to enhance the strength

## Slide 24: Adhesive failure comparison
Basis
Failures occur in time period of 45 ms
Patched variant
Failures occur in time period of 50 ms

## Slide 25: Material failure comparison
Basis
Patched variant
Failures occur in time period of 60ms
Failures occur in time period of 55ms
Plasticity has slightly increased
Displacement has decreased by 6.8 mm
Spotweld failure has decreased and adhesive failure has slightly increased but remain on the lower level
Material failure is on the same level

## Slide 26: Process simulation transfer – Thermal analysis results
Part with higher thickness cools slower than the part with lower thickness
Maximum temperature occurs in the region of the patch
Temperature distribution within GFRP is lower than the top part of Steel

## Slide 27: Process simulation transfer – Mechanical analysis results
No boundary condition has been applied
Overall displacement was found to be high with the maximum thickness patch as it cools down relatively slower
Maximum out-of-plane displacement of about 4.3 mm for 3 mm patch and 4.6 mm for 5 patch was found respectively
Load: Nodal temperatures from thermal analysis

## Slide 28: Process simulation transfer – Mechanical analysis results
The damage initiation criterion has already exceeded the maximum values in some areas
The patch thickness also plays an important role which leads to slightly different results

## Slide 29: Contents
  Hybrid plate overview and material model requirement
  Workflow and Simulation principle
          Hybrid plate process simulation
          Structural test and its validation
          Potential analysis in Toyota Camry
          Conclusion and future work

## Slide 30: Conclusion and scope for future work
Conclusion
A simulation method has been identified for the adapted process
A process history of the behavior of adhesive can be established
Different components can be analysed for the potential patching process so that weight reduction reduces cost and increases environmental benefits
Future work
An experimental verification of the fusion bonding incorporated adhesively bonded BIW components numerically calculated in this work is desirable
The mapping of the adhesive stiffness degradation from ABAQUS to PAM-CRASH solver must be done
It must also be validated for the different temperatures of the car which undergoes heating in the dryer from 23°C to 180°C

## Slide 31
Thank you for your attention

## Slide 32: References
Edmund Haberstroh and Michael Sickert. Thermal direct joining of hybrid plastic metal components. KMUTNB International Journal of Applied Science and Technology, Vol.7:29–34, 09 2014. doi: 10.14416/j.ijast.2014.07.002.
Robert Thomas, Fabian Fischer, and Maik Gude. Adhesives for increasing the bonding strength of in situ manufactured metal- composite joints. Proceedings of the Institution of Mechanical Engineers, Part D: Journal of Automobile Engineering, pages 1–14, 2020. doi: 10.1177/0954407020965759. URL https://doi.org/10.1177/0954407020965759.
Alexander Böttcher and Hermann Opdemom. Series-production adhesive process for hybrid components. Lightweight Design worldwide, Vol.12:48–53, 2019.
Larry.M. A guide to carbon fiber reinforced polymer repairs. 2016. URL https://www.vehicleservicepros.com/collision-repair/body-shop-and-repair/article/21191679/a-guide-to-carbon-fiber-reinforced-polymer-repairs
Claus-Peter Köth. Insight Automobilindustrie 2016 Leichtbau in der Automobilindustrie. Vogel Verlag. 2016.
Robert Georg Dietrich. Analyse der Wärmeausdehnungs-Inkompatibilität bei Klebverbindungen aus CFK, Stahl und Aluminium bei der Fertigung einer lackierten Karosserie. PhD thesis, Technische Universität München, Germany, 2017.
Theseus FE. https://www.theseus-fe.com/simulation-software/paint-dryer-simulation
Numerische abschätzung von eigenspannungen und bauteilverformungen in gesamtfahrzeugmodellen beim kleben im karosseriebau. Paderborner Symposium Fügetechnik (2006). https://www.theseus-fe.com/ths_content/publications/slides/20061129_slides_kleben-im-karosseriebau_prozess-simulation_de.pdf
Composite insert as a structural reinforcement for a-pillars. Continuousfiber- reinforced thermoplastic composites for lightweight car design, 10 2019. URL https://lanxess.com/en/Media/Press-Releases/2019/09/Composite-insert-as-a-structural-reinforcement-for-A-pillars

## Slide 33: References
10. Leif Ickert, Dieter Thomas, Thomas Tröster, and Lutz Eckstein. Beitrag zum fortschritt im automobilleichtbau durch belastungsgerechte gestaltung und innovative lösungen für lokale verstärkungen von fahrzeugstrukturen in mischbauweise.
FAT-Schriftenreihe 244, (244), 2012.
11. Niklas Günther, Michael Griese, Elisabeth Stammen, and Klaus Dilger. Modeling of adhesive layers with temperature-dependent cohesive zone elements for predicting adhesive failure during the drying process of cathodic dip painting. Proceedings of the Institution of Mechanical Engineers, Part L: Journal of Materials: Design and Applications, 233:146442071880600, 10 2018. doi:
10.1177/1464420718806005.
12. Three point bend test fixtures URL https://www.instron.com/de-de/products/testing-accessories/flexure-fixtures/three-point-bend-test-fixtures?region=Germany
13. Muhammad Anas Athar M.Sc. Experimental values of the GFRP laminate. 2021.
14. Hexcel. Mechanical properties of Redux® 677.URL https://www.hexcel.com/user_area/content_media/raw/HexBond_677_DataSheet.pdf
[2021; accessed 20-July-2021].
15. Manuel Längauer, Franz Brunnthaller, Gernot Zitzenbacher, Christoph Burgstaller, and Christoph Hochenauer. Modeling of the anisotropic thermal conductivity of fabrics embedded in a thermoplastic matrix system. Polymer Composites, 42, 01 2021. doi: 10.1002/pc.25958.

## Slide 34: References
16. Alexander Lion, Anton Matzenmiller, Gerson Meschut, Dominik Teutenberg, Patrick Kühlmeyer, and Christoph Liebl. Methodenentwicklung zur simulation und bewertung fertigungs- und betriebsbedingter klebschichtschädigungen
infolge temperaturwechselbeanspruchung. Forschungsvorhaben P878, Förderkennzeichen 369 ZN, 2014.
17. W. P. Goss. Thermal properties of wood and wood products.
18.David W. Green, Jerrold E. Winandy, and David E. Kretschmann. Mechanical properties of wood. wood handbook : wood as an engineering material. madison, wi : Usda forest service, forest products laboratory. General technical
report FPL ; GTR-113: Pages 4.1-4.45, 1999.
19.Young’s modulus: Modulus of elasticity of wood. URL https://amesweb.info/Materials/Youngs-Modulus-of-Wood.aspx [2021; accessed 20-July-2021].
20.Modulus of elasticity and Poisson’s coefficient of wood. URL https://www.sonelastic.com/en/fundamentals/tables-of-materials-properties/woods.html . [2021; accessed 20-July-2021].
21. Dušan Kecman. Bending collapse of rectangular and square section tubes. International Journal of Mechanical Sciences, Vol.25(9):623–636, 1983. ISSN 0020-7403. doi: https://doi.org/10.1016/0020-7403(83)90072-3. URLhttps://www.sciencedirect.com/science/article/pii/0020740383900723 Special
Issue Structural Crashworthiness Conference.

## Slide 35
Appendix

## Slide 36: Lightweight components
Hybrid front bumper [3]
Hybrid A-pillar [3]

## Slide 37: Why cooling procedure?
Different variables during paint drying process

## Slide 38: Why cooling procedure?
1
2
Heating phase
3
Holding phase
4
Cooling phase
Adhesive fracture [3]
Adhesive crack [3]
[6]
Deformation
Cohesive failure
Adhesive failure
Material failure
Highest stresses in adhesive layer occur during cooling because the adhesive is fully cured at this point and the relative displacements are just starting to decrease

## Slide 39: Thermal-stress analysis
An illustration of the sequentially coupled thermal-stress analysis
Two fields has to be determined in thermo-mechanical analysis
One field influences the other or both can influence each other
Can be solved by uncoupled heat transfer and then a displacement/stress analysis
In this problem, temperature does not depend on stress analysis
This is a common example of sequential multiphysics workflow
Temperature
Displacement
Load

## Slide 40: Steel plate cooling simulation
Cooling simulation model of the Steel component of the hybrid plate
Cooling simulation interpretation of Steel plate through a video

## Slide 41: Support plate cooling experiment
Steel
With Kapton tape(Thickness - 1.63 mm)
Material
Experimental duration
800 seconds
Temperature
Initial temperature – 180°C
Support plate With Kapton tape (Thickness - 1.73 mm)
Geometry & Measurement points
a = 300 mm, b = 240 mm
Experimental Method
Free convective cooling of Support plate with Kapton tape
Support plate with Kapton tape
Cooling experimental setup for support plate of the hybrid plate

## Slide 42: GFRP cooling experiment
Steel
Method
Free convective cooling of CFRP
Material
Experimental duration
1200 seconds
Temperature
Initial temperature – 180°C
Geometry & Measurement points
a = 230 mm, b = 230 mm
c = 300 mm, d = 240 mm
e = 5 mm, f = 36 mm, g = 34 mm, h =45 mm Kapton tape
Experimental Method
Free convective cooling of GFRP along with support plate
GFRP (Thickness – 2.09 mm)
Support plate (Thickness – 1.743 mm)
Cooling experimental setup for GFRP along with support plate of the hybrid plate

## Slide 43: Cooling experiment for individual components
Steel
Support plate
GFRP
Goal:
To record the temperature distribution of the individual components of the hybrid plate and to compare the results with FE results to obtain a justification
Cooling experiments for the individual components of the hybrid plate

## Slide 44: Steel cooling simulation setup
T2
T1
T3
The temperatures were measured at exactly same points as that of the experiment to compare the results

## Slide 45: Material properties – Thermal analysis
 | Density [ton/mm3] | Thermal conductivity [mW/mm K] |  |  | Specific heat capacity [mJ/ton K]
Steel | 7.85e-9 | 52 |  |  | 0.48e9
GFRP [15] | 1.6e-9 | k11 | k22 | k33 | 0.95e9
 |  | 4.5 | 0.67 | 0.67 | 
Support plate | 7.85e-9 | 52 |  |  | 0.48e9
Adhesive[16] | 1.2e-9 | 2 |  |  | 1.2e9
Wooden strip | 5.48e-10 | 0.14 |  |  | 1.63e9

## Slide 46: Material properties – Mechanical analysis
 | Young’s modulus [MPa] | Poisson’s ratio | Thermal expansioncoefficient [K-1]
Steel | 210000 | 0.3 | 1.3e-5
Support plate | 210000 | 0.3 | 1.3e-5
Wooden strip | 10000 | 0.4 | -
Temperature-dependent thermal expansion coefficient used for Bonding agent

## Slide 47: Material properties – Mechanical analysis
Tensile, shear and energy release rates used for bonding agent [11]
Temperature dependent elastic properties of Bonding agent

## Slide 48: Bilinear traction separation law
Temperature dependent behavior of cohesive zone elements [11]
Mechanical parameters of a bilinear traction separation law [11]

## Slide 49: Material properties – Mechanical analysis
Temperature dependent elastic properties of GFRP
Thermal expansion coefficient of GFRP

## Slide 50: Material properties – 3-point-bending
 | Young’s modulus [MPa] | Poisson’s ratio
Steel | 210000 | 0.3

## Slide 51: Material properties – GFRP, Adhesive
Elastic properties used for GFRP [13]
Tension |  |  | Shear |  | 
Modulus [MPa] | Strength [MPa] | Energy [mJ/mm2] | Modulus [MPa] | Strength [MPa] | Energy [mJ/mm2]
2500 | 50 | 1.5 | 860 | 50 | 1.5
Material parameters used for Redux 677 [14]

## Slide 52: Bending behavior
Bending collapse behavior of thin-walled structures [21]

## Slide 53: 3-point-bending results
Method
3-Point bending test
DIN EN ISO 14125
Material
DP980 (1.6 mm)
Temperature DP980_006 to 008 – With CDP process. Hardened by heating at 180°C for about 30 minutes
Tested at 18°C
Velocity
20 mm/min
Geometry
a = 10 mm, b = 80 mm, c = 15.05 mm, d = 1.6 mm

## Slide 54: 3-point-bending results
Method
3-Point bending test
DIN EN ISO 14125
Material
GFRP-PA6 (2.0 mm)
Temperature
Dried by heating at 80°C for about 15 hours
Tested at 20°C
Velocity
20 mm/min
Geometry
a = 10 mm, b = 80 mm, c = 15.07 mm, d = 2.0 mm

## Slide 55: 3-point-bending results

## Slide 56: Industrial process
Overview of CDP dryer process
Importance of cooling phase
Different variables during paint drying process [11]
Steel
[6]
[8]
Freshly painted car body positioned in paint-drying oven for curing [7]
Schematic representation of the temperature curve in a multi-material dryer process [6]
Aluminium/FRP
Deformation
Cohesive failure
Adhesive failure
Material failure
Stepwise heating Stepwise cooling
Heating zone
Cooling zone
[6]

## Slide 57: Hybrid plate process simulation – Mechanical analysis results
An average of 45% stiffness degradation is found within the adhesive
Also, in many regions the damage initiation criterion had already exceeded which indicates that more damage is likely
Steel adherend displaces in out-of-plane direction in production of DCB hybrid plate

## Slide 58: Mechanical analysis
Increase in damage initiation criterion along GFRP material orientation direction 1

## Slide 59: Process validation – Thermal analysis results
As expected the support plate tends to cool faster than the GFRP and has a temperature difference of about 3 degrees in the simulation

## Slide 60: Process validation – Mechanical analysis results
The validation from the simulation falls short of the experimental value by about 0.06 mm

## Slide 61: Process simulation transfer – Mechanical analysis results

## Slide 62: Spot weld failure comparison
Patched variant
Failures occur in time period of 25 ms
Spotwelds were added additionally to enhance the strength

## Slide 63: Adhesive failure comparison
Patched variant
Failures occur in time period of 50 ms

## Slide 64: Process validation simulation
Scaled by a factor of 300